R&D Laboratories Ltd

Unit U

Enkalon Industrial Estate

Antrim, Co Antrim BT414LJ

Tel: 028 94465753

**SALES SPECIFICATION SHEET**

**Sodium Silicate 75Tw**

**Alkali oxide Na2O:** 8.5% +/- 0.3% w/w

**Silicon dioxide:** 27.8% +/- 0.5% w/w

**Solids:** 36.3% +/- 0.7% w/w

**Weight Ratio:** 3.27 +/- 0.05

**Viscosity (at 20°C):** 70 – 120 mPas

**Relative density (20°C):** 38.6 – 40.1 °Be

**Specific Gravity:** 1.364 – 1.385 (at 20°C)

**Shelf life:** 2 years if stored in well sealed container and stored in cool place

**Comment:** Information on this specification is believed to be accurate at time of print and is given in good faith. It is however for the customer / end user to satisfy themselves as to the suitability for their own particular use. Accordingly, R&D Laboratories Ltd and its affiliated companies, give no warranty as to the fitness of the product for any particular purpose and implied warranty or condition (statutory or otherwise) is excluded, except to the extent that such exclusions are prevented by law. Freedom under patent or copyright and designs cannot be assumed.

Date prepared - 23/04/2013