R&D Laboratories Ltd

Unit U

Enkalon Industrial Estate

Antrim, Co Antrim BT414LJ

Tel: 028 94465753

**SPECIFICATION SHEET**

**Magnesium Carbonate – Heavy**

**Appearance:-** Fine White Powder

**Bulk density:-**  Approx. 800kg/m3

**Sieve Residue on 53micron:-** <6.0%

**LOI @ 9500C:-**  51.2%

**Typical Chemical analysis**

**MgO** 46.50%

**CaO** 0.80%

**Fe2O3** 0.05%

**SiO2** 0.45%

**Al2O3** 0.08%

Date prepared - 28/02/2013